Ref. No.: SRG/TDS/HR/2019							                                 Rev. No.: 00

TECHNICAL DATA SHEET

Hydantoin Resin (HR)

Hydantoin Resin (HR) is a class of bonding agent which provides a means for interacting a filler with a resin to form a composition.  HR is very suitable in the bonding an explosive substance with an oxidizer in composite propellant.

| Synonyms: | Diglycidyldimethylhydantoin |
| --- | --- |
| CAS No.: | 15336-81-9 |
| Molecular Formula: | C11H16N2O4 |
| Avg Mass: | 240.26 g/mol |
| IUPAC Name: | 5,5-dimethyl-1,3-bis(oxiran-2-ylmethyl)imidazolidine-2,4-dione |

SPECIFICATIONS FOR Hydantoin Resin (HR)

| Sr. No. | Characteristics | Specified Value |
| --- | --- | --- |
| 1. | Appearance | Homogeneous Viscous mass |
| 2. | Mass Fraction of Epoxy Group, % | ≥ 25 |
| 3. | Moisture Content, % | ≤ 0.1 |
| 4. | Mass Fraction of Volatile Substances % | ≤ 1.5 |
| 5. | Mass Fraction of Chloride Ion, % | ≤ 0.1 |
| 6. | Mass Fraction of Saponifiable Chlorine, % | ≤ 2.5 |
| 7. | Dynamic Viscosity at 40°C, Poise | ≤ 100 |
| 8. | Purity, % | > 98 |