Ref. No.: SRG/TDS/Specs/CS                                                                                                      Rev. No.: 00

TECHNICAL DATA SHEET

Monobasic Cupric Salicylate

(Cupric Salicylate)

Manufactured as per AS-3236 specification

| CAS No: | 62320-94-9 |
| --- | --- |
| Synonyms: | Hydroxy(2-hydroxybenzoato-O1,O2)copper |
| Molecular Formula: | C7H4CuO4 |
| Avg Mass: | 215.651 g/mol |
| IUPAC Name: | [3-Hydroxy-2-(hydroxy-kappaO)benzoato(2-)-kappaO]copper |

SPECIFICATION FOR

MONOBASIC CUPRIC SALICYALTE as per AS-3236 specifications

| Sr. No. | Properties | Specified Limits |
| --- | --- | --- |
| 1 | Total Lead, % | 39.8 – 40.7 |
| 2 | Beta Resorcylic Acid, % | 58.0 – 60.0 |
| 3 | Volatile matter, % | 3.0 max. |
| 4 | THF insoluble, % | 1.0 max. |
| 5 | Average particle size, mm | 10 |