Ref. No.: SRG/TDS/L2EH/2022                                                                                                     Rev. No.: 00

TECHNICAL DATA SHEET

LEAD 2-ETHYLHEXOATE

Manufactured as per MIL-L-17699 (Nord) specification

| CAS No: | 301-08-6 |
| --- | --- |
| Synonyms: | Lead(II) 2-ethylhexanoate Lead bis(2-ethylhexanoate) Hexanoic acid, 2-ethyl-, lead(2+) salt |
| Molecular Formula: | C16H30O4Pb |
| Avg Mass: | 494 g/mol |
| IUPAC Name: | bis(2-ethylhexanoate);lead(2+) |

SPECIFICATION FOR

LEAD 2-ETHYL HEXOATE as per MIL-L-17699 (Nord) dated August 24, 1953

| Sr. No. | Properties | Specified Limits |
| --- | --- | --- |
| 1 | Moisture and volatiles, % | 2.0, max |
| 2 | Alkalinity | NONE |
| 3 | Acidity to phenolphthalein as 2-Ethyl Hexanoic acid, % | 1.2, max |
| 4 | Total lead content, % | 40.5 – 42.5 |
| 5 | Viscosity | Z-8, min |
| 6 | Insoluble foreign material, % | 1.0, max |
| 7 | Color | Not darker than 7 by Gardner Standard |

Speciality Products Research Group offers the information contained in this technical data sheet solely for your information. We believe that all the information on this sheet is correct at the time of printing, but we make no warranty as to the accuracy of the data.