Ref. No.: SRG/TDS/LS/2015                                                                                                         Rev. No.: 00

TECHNICAL DATA SHEET

LEAD SALICYLATE (LS)

| CAS No: | 15748-73-9 |
| --- | --- |
| Synonyms: | Lead disalicylate, Lead, bis(2-(hydroxy-kappaO)benzoato-kappaO) Salicylic acid, lead(II) salt |
| Molecular Formula: | C14H10O6Pb |
| Avg Mass: | 481.0 g/mol |
| IUPAC Name: | bis(2-carboxyphenolate); lead (2+) |

SPECIFICATION FOR

LEAD SALICYLATE (LS) AS PER MIL-L-17700

| Sr. No. | Properties | Specified Limits |
| --- | --- | --- |
| 1 | Appearance | Cream-white to pure white powder |
| 2 | Lead Content, % | 42.2 – 43.7 |
| 3 | Total Salicylate Content, % | 55.0 – 59.0 |
| 4 | Volatile Matter at 105°C, % | 1.0 max. |
| 5 | Moisture, % | 1.0 max |
| 6 | Diethylene Glycol Insoluble Material, % | 2.50 max. |
| 7 | Free Salicylic Acid Content, % | 1.0 max |
| 8 | Retention on No. 325 Sieve, % | 0.5 max |

Speciality Products Research Group offers the information contained in this technical data sheet solely for your information. We believe that all the information on this sheet is correct at the time of printing, but we make no warranty as to the accuracy of the data.