Ref. No.: SRG/TDS/MCBR/2022                                                                                   Rev. No.: 00

TECHNICAL DATA SHEET

Copper Beta Resorcylate

(Monobasic Copper Beta Resorcylate)

| CAS No: | 70983-44-7 |
| --- | --- |
| Synonyms: | Monobasic Copper Beta Resorcylate, Benzoic acid, 2,4-dihydroxy-, copper salt, basic |
| Molecular Formula: | C14H10CuO8 |
| Avg Mass: | 369.772 g/mol |
| IUPAC Name: | Copper(2+) bis(2,4-dihydroxybenzoate) |

| SPECIFICATION FOR COPPER BETA RESORCYLATE Manufactured as per BC-3C005 specification |  |  |
| --- | --- | --- |
| Sr. No. | Properties | Specified Limits |
| 1 | Appearance | Fine Powder |
| 2 | Color | Brownish Grey |
| 3 | Copper Content, % | 26.0 min. |
| 4 | Volatile Matter, % | 4.5 max. |
| 5 | Acidity, mg KOH/gm | 30.0 max. |
| 6 | Particle Size, micron | < 2.0 |

Speciality Products Research Group offers the information contained in this technical data sheet solely for your information. We believe that all the information on this sheet is correct at the time of printing, but we make no warranty as to the accuracy of the data.