Ref. No.: SRG/TDS/M-LBR/2015                                                                                  Rev. No.: 00

TECHNICAL DATA SHEET

MONOBASIC LEAD BETA RESORCYLATE (MLBR)

| CAS No: | 20936-32-7 |
| --- | --- |
| Synonyms: | Lead Beta Resorcylate |
| Molecular Formula: | C7H5O4Pb |
| Avg Mass: | 360.3 g/mol |
| IUPAC Name: | Lead 2,4-dihydroxybenzoate |

SPECIFICATION FOR

MONOBASIC LEAD BETA RESORCYLATE

| Sr. No. | Properties | Specified Limits |
| --- | --- | --- |
| 1 | Appearance | Light Buff coloured Powder |
| 2 | Lead Content, % | 56±2.0 |
| 3 | Free acidity as Acetic Acid, % | 0.5 Max. |
| 4 | Volatile Matter at 105°C, % | 0.2 Max. |
| 5 | Water Soluble Sulphates | 0.05 Max. |
| 6 | Particle Size | < 75 µm |
| 7 | Water soluble Chloride as NaCl | 0.05 Max. |

Speciality Products Research Group offers the information contained in this technical data sheet solely for your information. We believe that all the information on this sheet is correct at the time of printing, but we make no warranty as to the accuracy of the data.