Ref. No.: SRG/TDS/PECH/2023							                Rev. No.: 00

TECHNICAL DATASHEET

POLYEPICHLOROHYDRIN (PECH)

Poly-Epichlorohydrin is used in the synthesis of Diol hydroxyl-terminated glycidyl azide polymer (GAP-diol). This polymer finds use in cast-cured ‘polymer-bonded explosive’ as well as cast-cured composite propellants and in gas generating compositions.

| CAS No: | 24969-06-0 |
| --- | --- |
| Synonyms: | Epichlorohydrin Polymer |
| Molecular Formula: | (C3H5ClO)n |
| IUPAC Name: | 2-(Chloromethyl)oxirane Polymer |

SPECIFICATIONS FOR

Poly-Epichlorohydrin (PECH)

| Sr No | Characteristics | Specified Limits |
| --- | --- | --- |
| 1 | Appearance | Clear Liquid |
| 2 | Physical State | Viscous Liquid |
| 3 | Odour | Mild Odour |
| 4 | Volatile Matter, % | < 0.5 |
| 5 | Moisture content, % | < 0.5 |
| 6 | Hydroxyl value, mg of KOH | 40 ± 5 |
| 7 | Viscosity @ 30°C, cP | 6400 - 6800 |
| 8 | Average Molecular Weight | 1000 – 1700 |