Ref. No.: SRG/TDS/TGAP/2022						                                 Rev. No.: 00

TECHNICAL DATA SHEET

TETRA FUNCTIONAL GLYCIDYL AZIDE POLYMER

Tetra Functional Glycidyl Azide Polymer (t-GAP) finds use in cast-cured ‘polymer-bonded explosive’ as well as cast-cured composite propellants and in gas generating compositions. Energetic binder such as t-GAP confers higher energy output when compared with non-energetic conventional binder like HTPB

| Synonyms: | Tetrafunctional Glycidyl Azide Polymer |
| --- | --- |
| CAS No.: | 143178-24-9 |
| Molecular Formula: | (C3H5O2)2(C3H5O2N3)n |
| Avg Mass: | >1900.00 g/mol |

SPECIFICATIONS FOR

Tetra Functional Glycidyl Azide Polymer (T-GAP)

| Sr. No. | Characteristics | Specified Value |
| --- | --- | --- |
| 1. | Appearance | Brown/Amber Color liquid |
| 2. | OH Value, mg KOH/gm | 80 ± 5 |
| 3. | Specific Gravity at 30°C | 1.3 ± 0.3 |
| 4. | Viscosity at 30°C, cP | 1500 - 2000 |
| 5. | Molecular Weight (VPO), Daltons | 1800 - 2000 |
| 6. | Nitrogen Content, % | 40 ± 2 |
| 7. | Moisture Content, %, Max. | 0.5 |
| 8. | Volatile Matter, %, Max. | 0.5 |

Speciality Products Research Group offers the information contained in this technical data sheet solely for your information. We believe that all the information on this sheet is correct at the time of printing, but we make no warranty as to the accuracy of the data.