Ref. No.: SRG/Spec/BPS/2025							                    Rev. No.: 01

TECHNICAL SPECIFICATION

BIS-PROPARGYL-SUCCINATE (BPS)

BPS acts as a curing agent analog to isocyanate in classical polyurethane systems. It can be varied in its content to influence on the mechanical properties of the cross-linked binders as measured by tensile tests. The mechanical properties can be adjusted in a wide range by varying the amount of BPS.

| Synonyms: | Di-2-propyn-1-yl succinate |
| --- | --- |
| CAS No.: | 4580-40-9 |
| Molecular Formula: | C10H10O4 |
| Avg Mass: | 194.184 g/mol |
| IUPAC Name: | 1,4-bis(prop-2-yn-1-yl) butanedioate |

| Sr No | Properties | Specification Limits |
| --- | --- | --- |
| 1. | Appearance | Dark Brown to Blackish Solid which easily melts to liquid above 34°C (@ room temperature) |
| 2. | Specific gravity @ 25°C | 1.10 – 1.30 |
| 3. | Melting Point, °C | 34.0 – 35.0 |
| 4. | FT-IR | 3258 (m), 2947(w), 2133 (w), 1723 (s), 1448 (m), 1418 (m), 1372 (m), 1311(s), 1152 (vs), 1018 (s), 961 (s), 911 (m), 798 (m), 737 (s), 680(vs); |