Ref. No.: SRG/TDS/DAG/2025						                                 Rev. No.: 00

TECHNICAL DATA SHEET

Diaminoglyoxime (DAG)

Diaminoglyoxime  is a key chemical intermediate primarily used in the synthesis of energetic materials, such as diaminofurazan (DAF). It is known for its role in creating high-energy-density compounds and acting as a ballistic modifier in propellants.

| Synonyms: | Diaminoglyoxim |
| --- | --- |
| CAS No.: | 2580-79-2 |
| Molecular Formula: | C2H6N4O2 |
| Avg Mass: | 118.095 g/mol |
| IUPAC Name: | 1-N',2-N'-dihydroxyethanediimidamide |

SPECIFICATIONS FOR

Diaminoglyoxime (DAG)

| Sr. No. | Characteristics | Specified Value |
| --- | --- | --- |
| 1. | Appearance | Fine Powder from pale yellow to yellow |
| 2. | Melting Point, °C | 200 – 204 |
| 3. | Purity. % | >95% |
| 4. | Density, g/cc | 1.7 – 2.0 |
| 5. | Moisture Content, % | < 0.5% |
| 6. | Solubility | Soluble in hot water |