Ref. No.: SRG/TDS/OEA/2022							               Rev. No.: 00

TECHNICAL DATA SHEET

OLIGO ETHER ACRYLATE (OEA)

Oligo Ether Acrylate is used for single base propellant as moderant to control the burning of propellants

| Synonyms: | Dimethacrylate-bis(triethylene glycol) phthalate (MGF-9) |
| --- | --- |
| CAS No.: | 2387-65-7 |
| Molecular Formula: | C28H38O12 |
| Avg Mass: | 566.59 |
| IUPAC Name: | Di(triethylene glycol)phthalate dimethacrylate |

SPECIFICATIONS FOR OEA

As per Russian Specification No.

TY-6-01-450-76 – TOP GRADE

| Sr. No. | Characteristics | Specified Value |
| --- | --- | --- |
| 1. | Appearance | Transparent Liquid having colour between yellow and dark brown |
| 2. | Viscosity at 20°C, Cp | 100 - 220 |
| 3. | Content of main substance, % | 98 min |
| 4. | Content of Hydroquinone, % | 0.03 – 0.070 |
| 5. | Content of water, % | 0.1 max |
| 6. | Saponification number, mg KOH | 384 min |
| 7. | Acid number, mg KOH | 1.0 max |
| 8. | Density, g/cm3 | 1.14 – 1.18 |